Slurries & Suspensions

Superabrasives and Abrasives Availability

and Application Chart

| Product | Description | # Shape and Size | Typical Applications |
| --- | --- | --- | --- |
| Monocrystalline Structure Diamonds Resin Bond System | These low cost diamonds are the most friable, and therefore will produce minimum scratches. | Irregular shape crystals. Available in variety of sizes from 0.1 through 120 um | This type of powder is recommended for general application when surface finish and processing cost are the most important such as steels, non-ferrous materials, carbides, and soft ceramics. Electronic grade diamonds are available with contamination level as low as 5 PPM. |
| Monocrystalline Structure Diamonds Metal Bond System | More expensive than resin bond powder. | Blocky shape crystals. Available in variety of sizes from 0.1 through 120 um | Recommended for specific applications when the material removal rate is most important and/or when resin bond powder is not performing up to standard, such as hard ceramics, glass, and stones. Electronic grade diamonds are available with contamination level as low as 5 PPM. |
| Polycrystalline Structure Diamond Powder | Super high friable diamond has multi edge system with hundreds crystals. | Particle shape varies from round to irregular depending on size. Available in the following ranges: 0-0.1; 0.05-0.15, 0.05-0.2, 0.5-1.0; 0-1.0; 0.5-1.5; 1-2; 0-2; 1-3; 2-4, 4-8, 0-6 um. | Recommended for applications where material removal rate and/or surface finish are more important than processing cost, and is impossible to achieve in any other way. Computer disks, optical parts, etc. Our DP3-SC Scratch Controlled powder is extremely suitable for electronic applications such as disc texturing and GMR Head lapping and polishing operations. |
| Boron Carbide Powder (Dry Classified) | Low friability Premium powder to be used instead of super friable diamonds. | Irregular to blocky shape. Available in sizes FEPA f40 through F1500 | Slicing of Silicon Carbide and Sapphire wafers, lapping and polishing of the hard ceramics where higher abrasive concentration can provide better flatness. Can provide up to 25% higher performance in slicing and lapping operations in comparison to wet classified powders. |
| Silicon Carbide Powder | This low cost material is the most friable of the carbon content abrasives. | Particles are 99% blocky shape. Available in FEPA sizes from F220 through F1500. | General Application where cost of raw materials is critical. Used for slicing, lapping and polishing of glass and germanium wafers and lapping of piston rings and gears. |

Bulletin UKA\Slurry/Abrasives R1 20814

3-3