Boron Carbide Powder

for Nuclear Applications

### Background

Boron is an important material for nuclear applications due to its high neutron absorption cross section (760 barn* at neutron velocity of 2200 m/sec).   The cross section of the B10 isotope in boron is considerably higher (3800 barn).  In addition, boron doesn’t contain decay products with a long half-life and high-energy secondary radioactive materials. Since pure boron is extremely brittle and difficult to produce in shapes (for example: control rods) boron carbide is the material of choice to use since it provides a high concentration of boron atoms in a strong and refractory form and is relatively easy to fabricate.  Boron Carbide powder is the best nuclear radiation absorber for high & low level nuclear waste containers.

UK Abrasives, Inc. is an ISO 9001:2000 registered producer of Boron Carbide powder and an NQA1 certified supplier capable of developing/fine tuning our powders to meet customer requirements.  Boron Carbide powder for nuclear applications is meticulously produced in separately controlled lots in strict compliance with NQA1 requirements.

### Typical Technical data

|  Appearance (dry state): | - Color | - Black |
| --- | --- | --- |
|  Chemical composition: | - Chemical formula: | - B4C Application |
|  | ## Grade | - NG (Nuclear) |
|  | - B + C min. | - 98 |
|  | - B (Boron) min. | - 76 |
|  | - C (Carbon) max. | - 24 |
|  | - B2O3 | - 0.1 |
|  | - Fe (Iron) max. | - 0.1 |
|  | - Si (Silicon) | - 0.01 |
|  | - N (Nitrogen) | - 0.5 |
|  | - Isotope B10 (atomic weight) | - 19.5-21.5% |
|  Physical data: | Knoop hardness (0.1) | 3000 |
|  | Mohs hardness | < 9.5 |
|  | Specific gravity: | 2.51 |
|  | Melting point: | 2723 F |
|  | Structure: | Monocrystalline |

Note: 1. Diamond’s Mohs hardness is 10.

2. * Barn is unit of area equal to 10-24 sq. centimeters, used to measure cross sections in nuclear physics.

# UK Abrasives Standard Products for Nuclear Applications

Our standard Nuclear Grade powders for various nuclear applications are shown below:

|  | UKA Grade | Average Particle Size | Typical Application | Notes |
| --- | --- | --- | --- | --- |
| 1. | NG112M | 112 micron | Additive to concrete | B<75% |
| 2. | NG36L | 36 micron |  | B<70% |
| 3. | NG24H | 24 micron | Nuclear Shielding Panels, Reaction Control Rods, Etc. | B>76% |
| 4. | NG24HE | 24 micron |  | B>76%% + Enhanced Heat Transfer Capability |
| 5. | NG100H | 100 micron |  | B>76% |
| 6. | NG100HE | 100 micron |  | B>76% + Enhanced Heat Transfer Capability |
| 7. | NG6H | 6 micron |  | B>76% |
| 8. | NG6HE | 6 micron |  | B>76% + Enhanced Heat Transfer Capability |

Notes: 1.  Custom products are available on request.

2.  Standard packaging in 100 lb (30 gal.) fiber drums.  Custom packaging is available on request.

Bulletin B4C Nuclear\01. Rev.1 (7.1.2002)

6-4